Nanoparticule de ZnO dopate cu Ca

Studenta : CARABULEA Maria-Carina

Specializarea: SIMONa

Grupa:1131A

Anul III

Coordonatori : s.i Ionela-Andreea NEACSU

Adrian Nicoara

Cuprins

1.Abstract	3

2.Introducere	4

3. Materiale	6

4.Sinteza nanoparticulelor	6

5. Proprietati	6

6.Utilizari	7

7.Concluzii	7

8.Citatii	7

# 1.Abstract

In the present work, undoped and Calcium (Ca) doped ZnO nanoparticles have been synthesised via hydrothermal method. In order to investigate the influence of Ca doping ratio on the ZnO nanoparticles physical properties we have varied the Ca doping ratio from 0 to 4%. X rays diffraction (XRD) and scanning electron microscopy (SEM) techniques have been used for the structural and morphological characterization of the synthesised nanoparticles. The optical characterization of the nanoparticles was achieved by the transmittance measurements. The XRD analysis reveals that the introduction of Ca in ZnO network causes the crystallographic parameters (lattice a, c and cell volume) enlargement, tensile strain creation and the crystallite size increase. The microscopy observations indicates that the prepared nanopowder becomes formed with homogeneously distributed spherical grains with increasing the Ca doping ratio. The optical band gap of the Ca doped ZnO is reduced with doping ratio due to the crystallite size increase and to the disorder creation with Ca introduction in ZnO network.[1]

# 2.Introducere

Nanostructured semiconductors have a great interest due to their unique physicochemical properties, which are different than their bulk [1], [2], [3]. In recent years ZnO, a multifunctional material, has attracted attention of many researchers due to their interesting properties suitable for optoelectronics and electrical applications such as, ultraviolet lasers devices, thin-film transistor, light-emitting diodes, solar cells, biological sensors . Zinc oxide (ZnO) is II–VI compound and n-type semiconductor owing a wide direct band-gap 3.36 eV at room temperature, high excitonic binding energy 60 meV, high electron mobility and high stability. It can be easily synthesised, it is non-toxic and environmental friendly.

ZnO nanoparticles can be synthesised by several processes including: spray-pyrolysis [9], sol–gel [10], hydrothermal synthesis [11], Co-precipitation [12], thermal decomposition [13] and combustion [14]. In the present work, hydrothermal method was used to synthesise ZnO nanoparticles. This technique allows the materials synthesis with a high homogeneity and purity . As well, it directly provides materials with various shapes through the reaction control. This method has several advantages such as easy to handle, low cost and a non-vacuum vessel use [10].

Doping is a valuable approach to tune ZnO nanoparticles properties. The physical and chemical properties of doped ZnO can be tailored by choosing the doping element. By this way, the energy band-gap and electronic structure of ZnO nanoparticles can be modulated allowing the control of their optoelectronic, photocatalytic and antimicrobial activity properties while maintaining its crystalline structure.[13], [14].

ZnO conductivity can be improved by appropriate doping [16], [17] by adding a small amount of III elements (Al, In, B) or IV element (Pb,Se). In this activity some metals have been tested as doping element of ZnO nanoparticles namely Al and In to control the electrical properties. Noble metals, such as gold and silver, have been also used as doping element, the photoluminescence properties of Au-doped ZnO nanoparticles were investigated [13].

It has been found that the diluted magnetic semiconductors formed by doping ZnO with transition metal such as (Fe, Mn, Co and Cr) exhibit interesting magnetic properties. It has been proved theoretically and experimentally that Group-I element (Li, Na) doping may produce p-type semiconductor through the creation of shallow acceptor levels in ZnO. As well, rare earth elements such as Nd, Gd, Er and Ce [16] have been used in ZnO nanoparticles for doping purpose. They modify the nanoparticles' photoluminescence emission and improve their photocatlytic activity. It has been outlined that doping ZnO nanoparticles with rare-earth elements (Eu, Tb, and La) influences their growth, leading to a decrease in their average crystallite size [17].

However, to the best of our knowledge, doping with II column element such Ca is less investigated, few reports are compiled [18]. This is at the motivation of ZnO Ca doping effect study.

The present work is an investigation of the effect of Ca doping on the properties of ZnO nanoparticles synthesised by hydrothermal method.

Calcium is a silvery-white, soft metal with significant antibacterial properties[2]

.

# 3. Materiale

# 4.Sinteza nanoparticulelor

Ca-doped ZnO nanoparticles were prepared using the hydrothermal technique.[2]

# 5. Caracterizare

# 6.Utilizari

# 7.Concluzii

In conclusion, undoped and Ca doped ZnO nanoparticles have been prepared using hydrothermal method. Ca doping effect on the physical properties of ZnO nanoparticles have been investigated. The structural analysis reveals that the introduction of Ca in ZnO network causes the ZnO network swelling yielding to the crystallographic parameters (lattice a, c and cell volume) enlargement, tensile strain creation, Zn-O bond length stretching and the crystallite size increase [1]

# 8.Referinte

[2]-Titanium surface functionalization with calcium-doped ZnO nanoparticles for hard tissue implant applications - ScienceDirect

[1]-Properties of calcium doped ZnO nanoparticles prepared by hydrothermal technique - ScienceDirect

Citatii